SECTION 06 42 00 – ACOUSDECK WALL™ / Non-Structural Acoustic Wood Wall Panel

- GENERAL

      - RELATED DOCUMENTS

        - Drawings and general provisions of the Contract, including General and Supplementary Conditions and Division 01 Specification Sections, apply to this Section.

      - SUMMARY

        - Section Includes:

          - ACOUSDECK WALL™.

          - Field finishing.

      - Related Requirements:

- {Specifier’s Note: Keep relevant sections below depending upon how the ACOUSDECK WALL™ panel is used on the Project.}

          - Section 01 81 13 “Sustainable Design Requirements.”

          - Section 05 12 00 “Structural Steel Framing” for coordination with structural steel frame where panels are used as a wrap.

          - Section 06 10 00 “Rough Carpentry” for substrates, nailers, and blocking.

          - Section 06 40 00 “Architectural Woodwork” for coordination with other architectural woodwork.

          - Section 09 91 00 “Painting” for field finishing of wood panels.

          - Section 09 93 00 “Staining and Transparent Finishing” for field finishing of wood panels.

- {↑ Specifier’s Note: Any paints, stains, coatings, or other field-applied finishes should be included in a Division 09 specification section.}

      - DEFINITIONS

        - ACOUSDECK WALL™: A non-structural, two-layer acoustic wood wall panel intended for interior finish and acoustic use only; not intended to resist imposed structural loads or to act as a shear or diaphragm element.

        - Backer Layer: The non-structural glued-laminated wood substrate layer of the panel, fabricated from wood laminations and providing the mounting substrate for the Non-Structural Acoustic Layer.

        - Non-Structural Acoustic Layer (NSAL): The exposed wood layer of the panel containing acoustic channels and sound-absorptive acoustic insulation infill, which provides the panel’s acoustic performance and finished appearance.

        - NRC: Noise Reduction Coefficient, determined in accordance with ASTM C423.

      - REFERENCE STANDARDS

- {Specifier’s Note: Keep relevant references below depending upon the applicable requirements for the Project.}

        - ANSI/AWI 0642 – Wood Paneling.

        - AWI 200 – Care and Storage.

        - ASTM C423 – Standard Test Method for Sound Absorption and Sound Absorption Coefficients by the Reverberation Room Method.

        - California Department of Public Health (CDPH) Standard Method v1.2 – Standard Method for the Testing and Evaluation of Volatile Organic Chemical Emissions from Indoor Sources Using Environmental Chambers.

        - [ASTM D7612 – Standard Practice for Categorizing Wood and Wood-Based Products According to Their Fiber Sources.]

FSC® Chain of Custody: SCS-COC-007899 | Trademark: FSC-C162183 | fsc.org/en

PEFC Chain of Custody: SCS-PEFC-COC-007899 | Trademark: PEFC/29-31-395 | www.pefc.org

SFI® Chain of Custody: SCS-SFI-COC-007899 | Trademark: SFI-01976 | forests.org
SFI marks are registered marks owned by the Sustainable Forestry Initiative Inc.

      - ACTION SUBMITTALS

        - Product Data: For each type of product.

          - Panel dimensions, tolerances, acoustic profile, and edge-profile details.

          - Product data for base layer wood laminations and for the Non-Structural Acoustic Layer, including species and appearance classification.

          - Product data for adhesives.

          - Product data for the acoustic insulation infill, including material composition, density, thickness, and fire-performance characteristics.

          - Product data for sealer/finish:

            - Product data for factory-applied sealer or finish, where specified.

            - Product data and application instructions for field-applied sealer or finish, where specified.

        - Acoustic Performance Documentation: Documentation of acoustic performance for the panel assembly, including Noise Reduction Coefficient (NRC):

          - Laboratory test reports in accordance with ASTM C423; or

          - Where laboratory testing is not available, submit a letter from a qualified independent acoustical consultant documenting expected acoustic performance based on comparable assemblies, material properties, and/or predictive modeling and/or indicative testing.

        - Samples: Provide a minimum of three samples, minimum 12-inch width by 12-inch length by typical panel thickness, for each species, acoustic-material combination and sealer/finish, demonstrating the range of variation to be expected in appearance of ACOUSDECK WALL™.

- {Specifier’s Note: Retain Sustainable Design Submittals language below only for Projects pursuing LEED certification (under version 4.1) or revise text for other sustainable design certification programs.}

        - Sustainable Design Submittals: Refer to Section 01 81 13 “Sustainable Design Requirements”.

          - LEED® MR Credit 3 – BPDO, Sourcing of Raw Materials:

            - Certified Wood: Documentation indicating percentage new wood, percentage Forest Stewardship Council® (FSC) and Chain-of-Custody (CoC) certificates for manufacturer and vendor. Include vendor invoice indicating FSC® and CoC.

            - Pilot Alternative Compliance Path - Legal Wood: Documentation of wood products from Certified Sources as defined by ASTM D7612 meeting following requirements:

              - 100 percent of all wood is verified to be from Legal (non-controversial) Sources as defined by ASTM D7612.

              - 70 percent of all wood used on the Project is from Responsible Sources as defined by ASTM D7612.

- {↑ Specifier’s Note: SFI Chain of Custody meets the requirements for both legal and responsible sources.}

          - IEQ Credit 2 - Low-Emitting Materials:

            - Interior Wet-Applied Coatings, Adhesives, Sealants: Certificate stating compliance with California Department of Public Health (CDPH) Standard Method V1.1-2010, including total volatile organic compounds (TVOC) range.

              - Include product data stating VOC content in g/L.

              - Include volume of material applied per product.

            - Insulation: Certificate stating compliance with California Department of Public Health (CDPH) Standard Method V1.1-2010, including total volatile organic compounds (TVOC) range.

{Specifier’s Note: Retain Sustainable Design Submittals language below only for Projects pursuing LEED certification (under version 5.0) or revise text for other sustainable design certification programs.}

        - Sustainable Design Submittals: Refer to Section 01 81 13 “Sustainable Design Requirements”.

LEEDv5 MRc3 – Low-Emitting Materials

ACOUSDECK WALL™ can contribute to LEED Environmental Quality EQc2 Occupant Experience Option 1, Path 1 Integrated Biophilic Design.

LEED MR Credit 4 – Building Product Selection and Procurement

Submit product documentation necessary to score eligible products in accordance with USGBC’s approved LEED v5 MRc4 multi-attribute scoring methodology. TIMBERLAB RESOLVE GLT™ can earn LEED Multi-attribute points in the following areas:

- Include manufacturer-provided documents or links to documents that demonstrate a multi-attribute score of at least three according to LEED v5 BD+C MRc4: Building Product Selection and Procurement.

      - QUALITY ASSURANCE

        - ACOUSDECK WALL™ shall be factory-manufactured under controlled conditions.

        - Adhesives shall be specifically formulated for interior architectural woodwork and shall be capable of producing a durable, uniform, and stable bond consistent with the fabrication and performance criteria required by AWI Standards for architectural woodwork and interior finishes.

      - DELIVERY, STORAGE, AND HANDLING

        - General: Comply with provisions in AWI 200 – Care and Storage.

        - ACOUSDECK WALL™ panels must be palletized for delivery and protected to prevent water intrusion and damage to the exposed acoustic face.

        - Store panels flat, elevated from grade, and under cover. Handle to prevent damage.

      - PROJECT CONDITIONS

        - Do not install ACOUSDECK WALL™ until the building is enclosed and ambient conditions are stabilized to service levels.

        - Acclimate panels a minimum of 48 hours prior to installation.

      - WARRANTY

        - Manufacturer’s standard one-year warranty against defects in materials and fabrication, excluding natural wood color and grain variations and damage due to improper storage, handling, installation, or maintenance.

- PRODUCTS

      - PERFORMANCE REQUIREMENTS

- {Specifier’s Note: Specify desired NRC requirement. Do not specify an NRC greater than 0.6; the maximum rated acoustic performance of ACOUSDECK WALL™ is 0.6 NRC.}

        - Acoustic Requirement: [ .X NRC ] in accordance with ASTM C423.

Average sound absorption coefficient in the 500Hz to 2kHz range: 0.7 minimum

- {Specifier’s Note: Include applicable sustainability requirements for the Project.}

        - Sustainability Requirements: Comply with Section 01 81 13 “Sustainable Design Requirements.”

      - MANUFACTURER

        - Basis-of-Design Product: ACOUSDECK WALL™ by Timberlab.

        - Manufacturer: Timberlab Laminators, LLC. P.O. Box 297, Drain, OR 97435; Office Phone: (503) 749-7500.

        - Substitutions: Not Permitted.

      - MATERIALS

        - Wood Species:

- {Specifier’s Note: Include Visual Face species options below as applicable. Verify availability per species at time of pricing.}

          - Visual Face Species (Non-Structural Acoustic Layer):

            - Standard Options:

              - [Douglas Fir (DF)]

              - [Southern Pine (SYP)]

              - [Spruce Pine Fir South (SPF South)]

            - Custom Options:

              - [Alaskan Yellow Cedar (AYC)]

              - [Port Orford Cedar]

              - [Oregon White Oak]

              - [Red Alder]

              - [Pacific Maple]

              - [Other wood species]

          - Backer Layer (non-visual face): Douglas Fir or other wood species acceptable to Manufacturer.

- {Specifier’s Note: If the Project has FSC® or SFI requirements, use the appropriate line for Certified Wood below. Verify availability of FSC® and SFI certification per species at time of pricing.}

          - Certified Wood: Input wood shall be certified as “FSC Mix Credit” according to FSC STD-01-001, “FSC Principles and Criteria for Forest Stewardship,” and to FSC STD-40-004, “FSC Standard for Chain of Custody Certification.”

          - Certified Wood: Input wood shall be certified as “SFI Credit” or “SFI 100% as calculated under the credit method” according to the “SFI 2022 Forest Management Standard” and the “SFI 2022 Chain of Custody Standard.”

        - Acoustic Insulation Infill:

          - [Grey/black fiberglass with black facing]

          - [Acoustic felt] in [color]

        - Adhesives

          - Moisture-resistant wood adhesives suitable for laminated wood panels.

      - ACOUSDECK WALL™  CONSTRUCTION

        - Dimensions:

          - Backer Layer: 0.67”

          - NSAL wood lamination layer: 1.375”

            - NSAL contains acoustic channels and factory-installed sound-absorptive acoustic insulation infill.

          - Overall Panel Thickness (Base Layer plus NSAL): 2”

          - Nominal Panel Size: 21” x 10’-0”

          - Squareness Tolerance: plus or minus 1/32 inch over panel width.

          - Length and Width Tolerance: plus or minus 1/32 inch in either direction.

        - Rating: Up to 0.6 NRC.

        - Acoustic Profile:

          - 1-UP – Acoustic channels at 5.25 inches on-center.

          - 2-UP – Acoustic channels at 2.625 inches on-center.

        - Configuration:

          - Two ply panel

            - The backer layer plies are oriented along the width of the panel.

            - The NSAL plies are oriented along the length of the panel.

          - Panels shall have one visual face, comprising the Non-Structural Acoustic Layer.

        - Edge Profile: Groove along long panel edges.

        - Appearance Classification: ACOUSDECK WALL™ finished to Architectural Appearance (AA) unless otherwise specified.

      - Finish

Finish Options:

          - Raw: Factory sanded to 150 grit, unfinished.

          - Factory applied finish: Clear conversion varnish

          - Field-applied finish: By others.

            - Apply finish per finish manufacturer’s instructions.

- EXECUTION

      - EXAMINATION

        - Verify that furring and substrates in areas to receive ACOUSDECK WALL™ are plumb, flat, and within tolerances required to achieve flush panel alignment. Report unsatisfactory conditions in writing.

        - Proceed with installation only after unsatisfactory conditions have been corrected.

      - PREPARATION

        - Refer to AWI 200 – Care and Storage for storage and protection prior to installation.

Coordinate furring, backing, and blocking, as needed (30” on-center vertically, minimum).

      - INSTALLATION

        - Installation by others.

        - Install per approved submittals and in accordance with the Contract Documents and AWI Standards for installation tolerances and substrate penetration.

          - Installers shall use fasteners suitable for installation of ACOUSDECK WALL™ to the substrate, based on substrate construction.

            - Use stainless or coated fasteners compatible with the finish.

            - Remove acoustic insulation infill as needed to locate fasteners inside acoustic channel. Reinstall acoustic insultation infill after fastening is complete.

              - Fasteners shall be countersunk.

          - Joints:

            - Shim, level, and align panels to produce flush, uniform joints consistent with AWI guidelines.

            - Install splines in edges groove provided to join panels.

              - Maintain uniform joint widths and alignment.

          - Do not force joints; address substrate tolerances first.

          - Non-Structural Use; do not use panels to support imposed loads or as shear or diaphragm elements.

      - FIELD FINISHING

        - [Field Finishing: Refer to Section 09 91 00 “Painting.”]

- {↑ Specifier’s Note: Field finishing should be in the painter’s scope. Final/top coat should be done on site and shall follow the coating manufacturer’s recommended surface prep.}

      - PROTECTION

        - Protect installed ACOUSDECK WALL™ panels from damage and moisture during construction. Temporary edge guards are recommended.

END OF SECTION